## Slide 1
Compression Moulding
Composite Manufacturing Process
High-volume production of thermoset and thermoplastic
composite parts using matched-die moulds and heat/pressure
Process | Materials | Mould Design | Applications | Quality

## Slide 2
Compression Moulding Process

## Slide 3
Mould Design & Construction

## Slide 4
Moulding Compounds & Materials

## Slide 5
Key Process Parameters
Critical Variables
Mould Temperature
130–170°C (thermoset) — controls cure rate and surface quality
Clamping Pressure
5–20 MPa — ensures complete cavity fill and fibre compaction
Closing Speed
Slow initial close prevents fibre wash; fast final consolidation
Charge Weight & Pattern
60–80% cavity coverage; pattern controls flow and knit lines
Cure Time
1–5 min (SMC) — dictated by wall thickness and resin reactivity
Breathing / Degassing
Brief mould open/close cycles to vent trapped volatiles
Typical Cycle Breakdown
Chart: 
| Charge Placement | Mould Closing | Curing | Demoulding & Trim
Cycle | 15 | 10 | 55 | 20
Total cycle: 2–6 min (SMC) | Up to 30 min (thick prepreg)

## Slide 6
Applications

## Slide 7
Common Defects & Remedies

## Slide 8
Advantages & Limitations
Advantages
High production volume (100k+ parts/year per tool)
Short cycle times (1–5 min for SMC/BMC)
Excellent surface finish (Class A achievable)
Complex 3D geometry with ribs, bosses, inserts
Low material waste (90–95% utilisation)
Consistent part-to-part quality
Suitable for large structural panels
Limitations
High tooling cost (hardened steel matched dies)
Limited to relatively simple geometries (no deep undercuts)
Flash removal / trimming adds secondary operations
Fibre orientation difficult to control precisely
Material shelf life limitations (SMC/BMC)
Part size limited by press tonnage capacity
Thermoset parts not recyclable (cross-linked)

## Slide 9
Compression Moulding vs. Other Processes
Feature | Compression Moulding | Injection Moulding | RTM / VARTM | Hand Layup
Cycle Time | 1–5 min | 0.5–2 min | 15–60 min | Hours
Fibre Length | Short–Continuous | Short only | Continuous | Continuous
Part Size | Small–Very Large | Small–Medium | Medium–Large | Any
Surface Finish | Class A | Excellent | Good | Variable
Tooling Cost | High | Very High | Medium | Low
Volume Suitability | 10k–500k+ | 100k+ | 100–10k | 1–100
Automation | High | Very High | Medium | Low

## Slide 10
Summary & Future Outlook
Key Takeaways
Compression moulding is the workhorse process for high-volume composite part production
SMC/BMC deliver Class A surface finish at automotive production rates
Matched-die tooling enables complex geometry with ribs, bosses, and inserts
EV battery housings and structural composites are driving renewed growth
Emerging Trends
Carbon fibre SMC for lightweight structural automotive parts
Thermoplastic compression moulding for recyclable composites
Hybrid overmoulding — combining compression + injection in one tool
Industry 4.0 process monitoring with in-mould sensors and AI control
Thank You | Questions & Discussion