## Slide 1
The Future of
Aerospace Materials
Next-Generation Materials for Ultra-Light Aircraft
Advanced composites, nano-reinforcements, and novel architectures
shaping the next era of aerospace structural design
Carbon Fibre | Hybrid Composites | Lattice Structures | Thermoplastics | Nano-Reinforcements | High-Temp Polymers

## Slide 2
Carbon Fibre Microstructure

## Slide 3
Hybrid Composites

## Slide 4
Lattice Structures

## Slide 5
Thermoplastic Composites for Aerospace
Why Thermoplastics?
Weldability
Resistance/induction welding eliminates fasteners — 20% weight saving on joints
Recyclability
Re-meltable matrix enables closed-loop recycling and end-of-life recovery
Toughness
10x higher fracture toughness than epoxy — superior impact/damage tolerance
Rapid Processing
No autoclave cure; stamp forming in minutes instead of hours
Shelf Life
No cold storage required — unlimited out-time for prepreg materials
Repairability
Local re-heating allows in-situ repair of damaged structures
Key Thermoplastic Matrix Systems
Matrix | Tg (C) | Tm (C) | Use Case
PEEK | 143 | 343 | Primary structure
PEKK | 160 | 305-360 | Fuselage clips
PPS | 90 | 280 | Leading edges
PEI | 217 | Amorph. | Interior panels
PA6/PA12 | 50-80 | 220-260 | Secondary struct.
Industry Adoption
Airbus A350 — CF/PEEK brackets and clips
Gulfstream G650 — thermoplastic rudder
Boeing 787 — PEI interior panels
Clean Sky 2 — TP welded fuselage demonstrators

## Slide 6
Nano-Reinforcements

## Slide 7
High-Temperature Polymers
150-250 C Service
BMI (Bismaleimide)
Tg ~ 250-320 C after post-cure
Processable like epoxies (prepreg)
Used on F-22 Raptor structures
Hot/wet Tg: 200 C+
Good microcrack resistance
Fighter aircraft skins, engine nacelles, brake ducts
250-350 C Service
Polyimide (PMR-15, HFPE-II)
Tg: 340-400 C (exceptional)
Long-term oxidative stability
GE F414 engine duct liners
Addition-type cure chemistry
Challenging processing (high Tg)
Engine bypass ducts, exhaust structures, missile components
350 C+ Frontier
Ceramic Matrix (CMC) / Hybrid
SiC/SiC CMCs: 1300 C capable
Oxide/Oxide CMCs: 1200 C
LEAP engine shrouds (CFM)
GE9X combustor liners
60% lighter than Ni superalloys
Turbine shrouds, combustor liners, thermal protection

## Slide 8
Material Performance Comparison
Chart: Specific Strength (kN.m/kg)
| Aluminium 7075 | Titanium Ti-6Al-4V | Steel 300M | CFRP UD Epoxy | CFRP UD PEEK | CFRP+CNT Nano-hybrid
Specific Strength (kN.m/kg) | 210 | 240 | 170 | 780 | 750 | 880
Chart: Max Service Temperature (C)
| Standard Epoxy | Toughened Epoxy | BMI Composite | Polyimide PMR-15 | PEEK Composite | SiC/SiC CMC
Max Service Temp (C) | 120 | 180 | 250 | 350 | 260 | 1300
4x
Higher specific strength of CFRP vs aluminium
10x
Temperature range extension with CMCs over epoxies
30%
Further improvement with nano-enhanced matrices

## Slide 9
Technology Readiness Roadmap
Current
UD CFRP/Epoxy
(Boeing 787, A350)
Standard prepreg
autoclave processing
Near-Term
2025-2030
Thermoplastic welded
structures (fuselage)
Nano-enhanced toughened
epoxy systems
Mid-Term
2030-2035
Hybrid CFRP/metal
lattice airframes
In-situ AFP/ATL with
real-time quality
Long-Term
2035+
CNT-reinforced primary
structure certification
CMC hot-section
integrated with airframe

## Slide 10
Summary and Outlook
Key Takeaways
Carbon fibre composites already deliver 4x specific strength vs metals — nano-enhancements push this further
Thermoplastic matrices enable welding, recycling, and rapid out-of-autoclave manufacturing
Hybrid composites and FMLs combine best properties of different material classes
Lattice/anisogrid structures offer up to 40% weight saving over conventional sandwich panels
High-temperature polymers and CMCs are extending composite use into engine hot sections
The Ultra-Light Future
Multi-functional materials — structures that sense, heal, and adapt
Digital material twins — AI-driven design from micro to macro scale
Bio-inspired architectures — mimicking natural lightweight structures
Sustainable composites — recyclable thermoplastics and bio-based resins
Certification by analysis — reducing the test pyramid with simulation
Thank You | Questions and Discussion